## Slide 1: Path Dependence of Artificial Phototropic Growth with Inclined Illumination Inputs
Ariel Struzyk
24 May 2024

## Slide 2: How Does Growth Respond to an Inclined Illumination Input?
?
α ≠ 0˚
α = 0˚
500 nm
Notes: Can this natural phototropic process be translated to direct material patterning during growth instead of a template

## Slide 3: Out-of-Plane Inclination Single Growth Step
α = 0˚
α = 30˚
α = 40˚
α = 45˚
α = 50˚
500 nm
Q = 960 mC cm-2

## Slide 4: Effect of Charge with a Single Growth Step (α = 0°)
Q = 960 mC cm-2
Q = 1920 mC cm-2
500 nm

## Slide 5: Effect of Charge with a Single Inclined Growth Step
Q = 960 mC cm-2
Q = 1920 mC cm-2
500 nm
α = 30°

## Slide 6: 2 Step History Effect
960 mC cm-2, α = 30°
960 mC cm-2, α = 45°
1920 mC cm-2, α = 30°
960 mC cm-2 + 960 mC cm-2, α = 30° → 45°
500 nm
α = 30˚
α = 45˚
α = 30˚
α1 = 30˚
α2 = 45˚

## Slide 7: 30° Distribution
960 mC cm-2, 30°
500 nm

## Slide 8: α = 30° and 45° Comparisons
Residual: 80%
960 mC cm-2, α = 30°
960 mC cm-2, α = 45°
500 nm

## Slide 9: α = 30° and 50° Comparisons
Residual: 135%
960 mC cm-2, α = 30°
960 mC cm-2, α = 45°
500 nm

## Slide 10: More 2 Step History Effect
960 mC cm-2 + 960 mC cm-2, α = 30° → 45°
960 mC cm-2 + 960 mC cm-2, α = 30° → -45°
500 nm
Future Progress:
Try to get the most overlap between 30° and another inclination
  Redo the photoshop of the 40° samples to compare to the 30° samples
  Make 25° and 35° samples and compare them to the 30°

## Slide 11: Future: Two Step Deposition with Negated Direction
45°, -45° (what angle is symmetrical, and nothing will change?)
α = 45˚
α = -45˚
+
=
α1 = 45˚
α2 = -45˚

## Slide 12: Future: Two Step Deposition with Negated Direction
Start skoto and move to photo: Is the structure nice? What gives a similar output?
α = 30˚
α = -60˚
+
=
α1 = 30˚
α2 = -60˚
Other idea: Pitch increases as inclination changes, tuning the 2nd step wavelength
500 nm

## Slide 13
α = 0˚
α = 40˚
α = 60˚
α = 20˚
Orientation / degrees
0
-20
40
20
-40
Orientation / degrees
0
-20
40
20
-40
Orientation / degrees
0
-20
40
20
-40
Orientation / degrees
0
-20
40
20
-40
a)
b)
d)
e)
α = 30˚
c)
Orientation / degrees
0
-20
40
20
-40

## Slide 14
All images should correspond to 1.45x1.45um area cropped. (except very old simulations are likely 1.415)
Normal: 100kx SEM inserted 7.5”x8.14”, cropped to 4”x4”
Madeline: Scale cropped image scaled to 4”x4”, cropped to 2.83”x2.83”
For 500 nm scale bars:
2.00 inch image: 0.688 inch scale bar
2.25 inch image: 0.773 inch scale bar
2.50 inch image: 0.859 inch scale bar
2.75 inch image: 0.945 inch scale bar
3.00 inch image: 1.031 inch scale bar
3.50 inch image: 1.203 inch scale bar
4.00 inch image: 1.375 inch scale bar

## Slide 15: Potential Study
May 24th 2024
Ariel Struzyk

## Slide 16: Figures from term report

## Slide 17: Apparent Skototropic Growth Observed for Illumination at Near-Normal Incidence at λavg = 727 nm
500 nm
α = 0˚
α = 30˚
α = 10˚
α = 20˚

## Slide 18: Phototropic Growth Observed for Illumination at Significantly Off-Normal Incidence at λavg = 727 nm
500 nm
α = 70˚
α = 50˚
α = 60˚
α = 40˚