## Slide 1: Wetting: Research Ideas and Direction
Zoe Readi-Brown

## Slide 2: What’s Been Done?
Various structures achieves with photolithography
Nanowire wettability
  Locking and pinning
Laser patterning
J. Chung, et al., Soft Matter 2007
E. Fadeeva, et al., European Conference on Lasers and Electro-Optics, 2013
W. Wang, et al., Journal of Colloid and Interface Science 2024
SA > 90o
180o

## Slide 3: First: A General Survey of Squigz Wettability
Experiments:
  Unpolarized
    400 – 927 nm
  Vertically Polarized
    400 – 927 nm
  Dark Growth
Functionalization of each growth
  With several non-polar and polar thiol-ligated compounds

## Slide 4: A spectrum of achievable wettability in squigz
Hydrophillic
Hydrophobic
Dark Growth
Dark Growth
w/ non-polar func.
Dark Growth
w/ polar func.
Unpolarized Growth
Unpolarized Growth
w/ polar func.
Unpolarized Growth
w/ non-polar func.
Vert. Polarized Growth 800 nm
Vert. Polarized Growth 927 nm
Vert. Polarized Growth 800 nm
w/ non-polar func.
Vert. Polarized Growth 800 nm
w/ polar func.
Vert. Polarized Growth 927 nm
w/ non-polar func.
Vert. Polarized Growth 927 nm
w/ polar func.

## Slide 5: Idea 1: Lincoln Logs and the Wenzel State
B. Sadtler, et al., PNAS 2013

## Slide 6: Idea 2: Selective Chemical Etching
Selectively deposit different metals on tips and sides of squigz
  Two different materials = two separate wetting environments
    How would that affect the movement of water on the surface?

## Slide 7: Idea 3: Locking and Pinning with Tilted Growth
Sarah has done some preliminary measurements
  Did not achieve locking and pinning
If the surface hydrophilicity can be changed, the Wenzel state may be accessible, which could allow for locking and pinning
While it has been published in other structures, squigz are faster, cheaper, and easier to reproduce and scale

## Slide 8: Long Term?
Patterned Growth with DMD (digital mirror device), as previously presented
Patterning with 2 separate growths that have distinct wetting ability can have numerous effects
  Guiding of water along surface
  Anti-fogging possibility if hydrophyllic and hydrophobic surfaces exis