## Slide 1: Light-guided electrodeposition of non-noble catalyst patterns for photoelectrochemical hydrogen evolution
Sung Yul Lim, Yang-Rae Kim, Kyungyeon Ha, Jong-Kwon Lee, Jae Gyeong Lee, Woohyuk Jang, Jin-Young Lee, Je Hyun Bae and Taek Dong Chung
Zoe Readi-Brown
Energy & Environmental Science, 2015

## Slide 2: Light-guided spatially selective electrodeposition on a-Si at 632.8 nm
Pt4+ + 4e-  Pt0

## Slide 3: Minimal change occurs before and after the Pt nanoparticles are washes, demonstrating their adherence to the oxide surface

## Slide 4: DMD dynamic mark system for irreversible patterned electrodeposition
Pt4+ + 4e-  Pt0

## Slide 5: No platinum plating with no aqueous platinum ?!?
Pt4+ + 4e-  Pt0

## Slide 6
Ni-Mo!

## Slide 7: No Dory tho 

## Slide 8: Ni-Mo deposition by pulsing reveals roughened conformal layer with 5.7 Ni:Mo ratio

## Slide 9: More reduction potential pulses at -0.9 V (vs. Ag/AgCl) applies for 10s creates thicker Ni-Mo layer
100 nm
Ni2+ + Mo7+ + 9e-  Ni-Mo

## Slide 10: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2

## Slide 11: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2

## Slide 12: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2

## Slide 13: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2
X

## Slide 14: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2
X
X

## Slide 15: In spotted Ni-Mo systems, the number of dots on the surface increases current density to a point
2H+ + 2e-  H2
X
X
X

## Slide 16: Electrons collected at metal
A
Au3+ + 3e-  Au

## Slide 17: Movement of substrate during deposition creates smearing effect

## Slide 18: Spacing and diameter of Ni-Mo spots plateau with added area
2H+ + 2e-  H2

## Slide 19: Virtually no hydrogen evolution occurs with bare a-Si
2H+ + 2e-  H2

## Slide 20: Charge passed linearly proportional with illuminated area, pattern and illumination are 1 to 1

## Slide 21: Light absorption closest to initial Ni-Mo deposition causes more hydrogen evolution
2H+ + 2e-  H2

## Slide 22: As the pitch of Ni-Mo pattern/SiOx/a-Si changes with a constant Ni-Mo diameter, the total spectral reflectance changes

## Slide 23: Need to get our X-Ray Vision Ready!

## Slide 24: Independent photovoltaic and electrolyzer separates light absorption and chemical catalysis
Nocera, Inorg. Chem. 2009

## Slide 25
Nocera, Inorg. Chem. 2009